## Slide 1
Annual Summary of Molten Metal Incidents in 2022
September 2023

## Slide 2
Explosion Rating Force Criteria
TABLE 1. Explosion Rating Force Criteria Sep. 2023
Guidelines | Force 1 | Force 2 | Force 3
Property Damage | None | Minor | Considerable
Light | Minimal | Flash | Intense
Sound | Short cracking | Loud Report | Painful
Vibration | Short and sharp | Brief rolling | Massive structural
Metal Dispersion | <15 feet | >15 to 50 feet | >50 feet
Low
Severe

## Slide 3
FIGURE 1. Incidents Reported For The Period 1981 – 2022 Sep. 2023
Incidents by Year 1981 – 2022 (Total 4537)

## Slide 4
FIGURE 2. Incidents By Force Level 1981 – 2022 Sep. 2023
Incidents by Force Level 1981 – 2022 (Total 4537)

## Slide 5
FIGURE 3. Incidents By Force Levels 2 & 3 For 1981 – 2022 Sep. 2023
Incidents by Force Levels 2 & 3 1981 – 2022

## Slide 6
FIGURE 4. Force 3 Incidents For 1981 – 2022 Sep. 2023
Force 3 Incidents Only 1981 – 2022
5 Yr. Avg.: 1.0
10 Yr. Avg: 0.8
2.7

## Slide 7
FIGURE 5. Incidents By Force Level 1981 – 2022 Sep. 2023
Incidents by Force Level 1981 – 2022 (Total 4537)

## Slide 8
FIGURE 6. All Force Levels By Percentage 1981 – 2022 Sep. 2023
All Force Levels by Percentage 1981 – 2022

## Slide 9
Injuries from Incidents 1981 – 2022 (Total 1628)
FIGURE 7. Injuries From Incidents For 1981 – 2022 Sep. 2023

## Slide 10
FIGURE 8. % Injuries/Total Annual Incidents 2001 – 2022 Sep. 2023
Chart: 
| 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
 | 0.38971 | 0.49091 | 0.375 | 0.22464 | 0.25294 | 0.39669 | 1.2054 | 0.57831 | 0.47619 | 0.22353 | 0.34951 | 0.39655 | 0.27059 | 0.28037 | 0.32184 | 0.092308 | 0.044199 | 0.15294 | 0.090361 | 0.047619 | 0.071429 | 0.065657
121%
% Injuries per Total Annual Incidents 2001 – 2022 (Total 856 Injuries)

## Slide 11
Average # of Injuries / Year from Explosions
Chart: 
| Avg. Fatal /Yr | Avg. Serious / Yr | Avg Minor /Yr. | Avg Total /Yr.
2001-2015 | 2.3333 | 7.2 | 38.6 | 48.1333
2016-2022 | 1.1429 | 2.1429 | 10.5714 | 13.8571
FIGURE 9. Avg. # Injuries / Yr. For 2001-2015 & 2016-2022 Sep. 2023

## Slide 12
Injuries by Severity – Total 1628 1981 – 2022
FIGURE 10. Injuries By Severity For 1981 – 2022 Sep. 2023

## Slide 13
Injury Levels by Percentage 1981 - 2022
FIGURE 11. Injuries Levels By Percentage For 1981 – 2022 Sep. 2023

## Slide 14
Injury Risk per 100 Explosions 1981 - 2022
FIGURE 12. Injury Risk Per 100 Explosions For 1981 – 2022 Sep. 2023

## Slide 15
FIGURE 13. Fatalities From Explosions For 1981 – 2022 Sep. 2023
Fatalities from Explosions 1981 - 2022
Avg # Fatals Last 10 Yrs – 0.9

## Slide 16
Force Level Incidents by Operation – 2022
FIGURE 14. Force Level Incidents By Operation For 2022 Sep. 2023

## Slide 17
Force Level Incidents by Operation
1980 – 2022
FIGURE 15. Force Level Incidents By Operation For 1980 – 2022 Sep. 2023

## Slide 18
Melting Injuries and Incidents
1990 – 2022 (Total 334 Injuries)
FIGURE 16. Melting Injuries and Incidents 1990 – 2022 Sep. 2023
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Melting Injuries | 20 | 6 | 8 | 24 | 25 | 6 | 6 | 21 | 1 | 12 | 4 | 8 | 10 | 6 | 14 | 6 | 8 | 91 | 10 | 3 | 1 | 0 | 1 | 1 | 37 | 0 | 2 | 1 | 1 | 1 | 0 | 0
Melting Incidents | 54 | 35 | 38 | 67 | 42 | 42 | 25 | 27 | 29 | 22 | 56 | 45 | 42 | 35 | 40 | 39 | 31 | 27 | 27 | 14 | 20 | 14 | 27 | 31 | 51 | 39 | 68 | 46 | 65 | 55 | 55 | 74

## Slide 19
Melting Injuries per Incidents
1990 – 2022
FIGURE 17. Melting Injuries Per Incidents 1990 – 2022 Sep. 2023
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Melting Injuries / Incident | 0.37037 | 0.17143 | 0.21053 | 0.35821 | 0.59524 | 0.14286 | 0.24 | 0.77778 | 0.034483 | 0.54545 | 0.071429 | 0.17778 | 0.2381 | 0.17143 | 0.35 | 0.15385 | 0.25806 | 3.3704 | 0.37037 | 0.21429 | 0.05 | 0 | 0.037037 | 0.032258 | 0.72549 | 0 | 0.029412 | 0.021739 | 0.015873 | 0.018182 | 0 | 0
2007 Rate – 3.4 Due to Force 3 China Explosion w/ 84 Total Injuries, Including 16 Fatalities

## Slide 20
Casting Injuries and Incidents
1990 – 2022 (Total 358 Injuries)
FIGURE 18. Casting Injuries and Incidents 1990 – 2022 Sep. 2023
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Casting Injuries | 20 | 15 | 4 | 7 | 9 | 12 | 9 | 16 | 27 | 18 | 20 | 19 | 17 | 10 | 6 | 8 | 15 | 20 | 13 | 15 | 6 | 4 | 0 | 6 | 2 | 14 | 1 | 16 | 8 | 3 | 8 | 10
Casting Incidents | 55 | 28 | 29 | 19 | 22 | 29 | 21 | 17 | 19 | 22 | 44 | 30 | 38 | 57 | 44 | 58 | 36 | 45 | 23 | 20 | 30 | 24 | 32 | 31 | 76 | 116 | 75 | 71 | 62 | 66 | 59 | 93

## Slide 21
Casting Injuries per Incidents
1990 – 2022
FIGURE 19. Casting Injuries Per Incidents 1990 – 2022 Sep. 2023
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Casting Injuries / Incident | 0.36364 | 0.53571 | 0.13793 | 0.36842 | 0.40909 | 0.41379 | 0.42857 | 0.94118 | 1.4211 | 0.81818 | 0.45455 | 0.63333 | 0.44737 | 0.17544 | 0.13636 | 0.13793 | 0.41667 | 0.44444 | 0.56522 | 0.75 | 0.2 | 0.16667 | 0 | 0.19355 | 0.026316 | 0.12069 | 0.013333 | 0.22535 | 0.13115 | 0.047619 | 0.13559 | 0.108

## Slide 22
Transfer Injuries and Incidents
1990 – 2022 (Total 238 Injuries)
FIGURE 20. Transfer Injuries and Incidents 1990 – 2022 Sep. 2023
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Transfer Injuries | 3 | 8 | 0 | 0 | 3 | 13 | 13 | 4 | 6 | 9 | 12 | 17 | 34 | 22 | 4 | 18 | 13 | 10 | 16 | 8 | 2 | 2 | 0 | 7 | 3 | 0 | 3 | 8 | 4 | 3 | 2 | 3
Transfer Incidents | 13 | 8 | 11 | 16 | 8 | 15 | 14 | 17 | 11 | 18 | 36 | 45 | 60 | 48 | 34 | 50 | 36 | 23 | 20 | 18 | 20 | 3 | 5 | 27 | 20 | 18 | 23 | 40 | 23 | 19 | 22 | 21

## Slide 23
Transfer Injuries per Incidents
1990 – 2022
FIGURE 21. Transfer Injuries Per Incidents 1990 – 2022 Sep. 2023
Chart: 
| 1990 | 1991 | 1992 | 1993 | 1994 | 1995 | 1996 | 1997 | 1998 | 1999 | 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Transfer Injuries / Incident | 0.23077 | 1 | 0 | 0 | 0.375 | 0.86667 | 0.92857 | 0.23529 | 0.54545 | 0.5 | 0.33333 | 0.37778 | 0.56667 | 0.45833 | 0.11765 | 0.36 | 0.36111 | 0.43478 | 0.8 | 0.44444 | 0.1 | 0.66667 | 0 | 0.25926 | 0.15 | 0 | 0.13043 | 0.2 | 0.17391 | 0.15789 | 0.090909 | 0.14286

## Slide 24
74 Melting Explosions – 2022
FIGURE 22. Melting Explosions By Cause For 2022 Sep. 2023
Major Causes
Wet & Oxidized: Scrap, Sows, RSI
Wet Alloy Additions: Mg
Induction Furnace Failure – Force 2

## Slide 25
Melting Explosions – Charge Material Involved
1980 – 2022
FIGURE 23. Melting Explosions By Charge Material 1980 – 2022 Sep. 2023

## Slide 26
93 Casting Explosions – 2022
FIGURE 24. Casting Explosions For 2022 Sep. 2023
5 – Strip / Coil Casting

## Slide 27
DC/HDC/EMC Explosions by Cast Segment
1980 – 2022
FIGURE 25. Casting Explosions By Cast Segment 1980 – 2022 Sep. 2023

## Slide 28
Major Causes of 93 Casting Incidents – 2022
FIGURE 26. Major Causes of Casting Incidents For 2022 Sep. 2023
DC Start-up Issues: Wet Starting Blocks, Wet Equipment / Launder, Butt Curl – Hang-ups, Bleed-outs, Equipment Failures
DC Steady State Issues: Bleed Out – Surface Tears
DC Termination Issues: Wet / Rusty Drain Pan, Ingot Head Under Water, Metal on Floor
Strip / Coil Casting Termination Issues: Wet / Rusty Drain Pan
Sow / Mold Casting Issues: Wet / Cracked Molds, Wet Refractory, Equipment & Wet Tools

## Slide 29
Major Causes of Casting Explosions
2015 – 2022
FIGURE 27. Casting Explosions by Major Causes 2015 – 2022 Sep. 2023
Chart: 
| Sow Casting - Wet / Cracked / Rusty Molds | DC Cast Start - Excessive Curl / Hang-up / Bleed-out | Equipment Failure / Maint. Issue / Set-up | End of DC Cast & Aborts - Wet / Rusty Drain Pan | DC Cast Start - Wet / Rusty Bottom Block | Wet Refractory or Equipment | Ingot Head Under Water





 | 202 | 55 | 44 | 44 | 33 | 32 | 10

## Slide 30
Major Causes of Force 2 & 3 Casting Explosions
2015 – 2022
FIGURE 28. Casting Explosions by Major Causes 2015 – 2022 Sep. 2023
Chart: 
| DC Cast Start - Excessive Curl / Hang-up / Bleed-out | End of DC Cast & Aborts - Wet / Rusty Drain Pan | DC Cast Start - Wet / Rusty Bottom Block | Sow Casting - Wet / Cracked / Rusty Molds | Equipment Failure / Maint. Issue | Ingot Head Under Water
 | 16 | 14 | 9 | 8 | 5 | 3

## Slide 31
Major Causes of 22 Transfer Explosions – 2022
FIGURE 29. Causes of Transfer Explosions For 2022 Sep. 2023
13 - Wet Hand or Furnace Tools, Equipment
9 - Wet / Rusty Drain or Skim Pan
1 – Metal on Floor

## Slide 32
Transfer Explosions by Equipment
1980 – 2022 (Total 884)
FIGURE 30. Transfer Explosions by Equipment 1980 – 2022 Sep. 2023

## Slide 33
Major Causes of Transfer Explosions
2008 – 2022 (w/o 2011)
FIGURE 31. Transfer Explosions – Major Causes 2008 – 2022 Sep. 2023
Chart: 
| Wet / Rusty Drain Pan | Wet Tools | Wet Refractory or Equipment | Wet Floor / Spill
 | 134 | 116 | 86 | 22

## Slide 34
Major Causes of Force 2 & 3 Transfer Explosions
2008 – 2022 (w/o 2011)
FIGURE 32. Transfer Explosions – Major Causes 2008 – 2022 Sep. 2023
Chart: 
| Wet / Rusty Drain Pan | Wet Refractory or Equipment | Wet Floor / Spill
 | 15 | 6 | 4

## Slide 35
13 Injuries by Operation – 2022
FIGURE 33. Injuries By Operation For 2022 Sep. 2023

## Slide 36
1625 Injuries by Operation:
1980 – 2022
FIGURE 34. Injuries By Operation For 1980 – 2022 Sep. 2023

## Slide 37
Melting Explosions By Month
2017 – 2022
FIGURE 35. Melting Explosions By Month 2017 – 2022 Sep. 2023
Chart: 
| Sep | Oct | Nov | Dec | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug
2020 + 2021 | 9 | 7 | 7 | 4 | 10 | 23 | 13 | 4 | 4 | 6 | 8 | 4

## Slide 38
Casting Explosions By Month
2017 – 2022
FIGURE 36. Casting Explosions By Month 2017 – 2022 Sep. 2023
Chart: 
| Sep | Oct | Nov | Dec | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug
 | 23 | 16 | 22 | 19 | 16 | 10 | 18 | 15 | 17 | 21 | 14 | 19

## Slide 39
Transfer Explosions By Month
2017 – 2022
FIGURE 37. Transfer Explosions By Month 2017 – 2022 Sep. 2023
Chart: 
| Sep | Oct | Nov | Dec | Jan | Feb | Mar | Apr | May | Jun | Jul | Aug
 | 6 | 10 | 6 | 11 | 6 | 6 | 7 | 10 | 2 | 4 | 5 | 9

## Slide 40
Force Level By Process Plant – 2022
FIGURE 38. Force Level By Process Plant Reported For 2022 Sep. 2023

## Slide 41
Force Level By Process Plant
1980 – 2022
FIGURE 39. Force Level By Process Plant Reported For 1980 – 2022 Sep. 2023

## Slide 42
Reduction Plant
Main Causes of 79 Incidents – 2022
FIGURE 40. Reduction Plant Incidents Summary 2022 Sep. 2023
Melting Incidents | Casting Incidents
2 – Wet Tool 1 - Wet Charge: Scrap / Sow 1 - Wet Mg | Sow Casting: 33 - Cracked, Wet or Rusty Molds 4 - Undocumented 3 - Wet Tool, Equip, Refractory 1 -Termination - Overflow on Wet Floor 1 - Thermite w/ Rust
 | VDC – Billet & Slab 3 -Termination - Wet/Rusty Drain Pan 3 –Start-up – Wet Refractory / Equip. 2 - Termination - Overflow on Wet Floor 1 – Start-up – Wet Starting Block

## Slide 43
Reduction Plant
Main Causes of 79 Incidents – 2022
FIGURE 41. Reduction Plant Incidents Summary 2022 Sep. 2023
Transfer Incidents | Reduction Cell
4 - Wet Tools & Equipment 2 – Wet / Rusty Drain Pan | 4 – Wet Tools 3 - Tap-Out on Wet Floor 1 - Wet Tabular
 | 1 - Wet Tool 1 - Water Bottle
 | 1 - Anode into Wet Tub
 | 1 – Bath into Wet Tub

## Slide 44
Recycling Plant
Main Causes of 49 Incidents – 2022
FIGURE 42. Recycling Plant Incidents Summary 2022 Sep. 2023
Melting Incidents | Casting Incidents
29 - Wet Charge: Scrap, RSI, Sow, Dross 1 - Oxidized Mg | Sow Casting: 3 - Wet or Rusty Molds 4 - Wet Drain Pan
Transfer Incidents 4 - Wet / Rusty Drain Pan 3 - Wet Tools & Sample Mold | VDC – Billet: 1 - Start-up – Wet Starting Block

## Slide 45
Reduction Plant Injuries & Incident Causes – 2022
FIGURE 43. Reduction Plant Injuries By Operation 2022 Sep. 2023
6 Minor Injuries
3 – Wet Sampling Tools
2 – Wet Sow Molds
1 – Wet Starting Block; Billet

## Slide 46
Rolling Plant Injuries – 2022
FIGURE 44. Rolling Plant Injuries By Operation 2022 Sep. 2023
6 Minor Casting Injuries
3 – Start-up - Bleed-outs
2 – Termination - Wet / Rusty Drain Pan
1 – Start-up - Excessive Curl

## Slide 47
Extrusion Plant Injuries – 2022
FIGURE 45. Extrusion Plant Injuries By Operation 2022 Sep. 2023
1 – Minor Casting Injury Due to Ingot Hang-up at Start

## Slide 48
Recycling Plant Injuries – 2022
FIGURE 46. Recycling Plant Injuries By Operation 2022 Sep. 2023
No Injuries from 43 Force 1 & 5 Force 2 Incidents!

## Slide 49
Injury Severity by Process Plant – 2022
FIGURE 47. Injury Severity By Process Plant – 2022 Sep. 2023

## Slide 50
Injury Severity by Process Plant
1980 – 2022
FIGURE 48. Injuries Severity By Plant Reported For 1980 – 2022 Sep. 2023

## Slide 51
Reduction & Recycling Plant Incidents, Injuries / Incident Rate
2012 – 2022
Chart: Reduction Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Incidents | 40 | 55 | 78 | 119 | 139 | 84 | 87 | 51 | 66 | 50 | 78
Injuries | 19 | 20 | 21 | 49 | 6 | 5 | 7 | 4 | 2 | 2 | 6
Injury/ Incident Rate | 0.475 | 0.36364 | 0.26923 | 0.41176 | 0.043165 | 0.059524 | 0.08046 | 0.078431 | 0.030303 | 0.04 | 0.076923
Chart: Recycling Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Incidents | 7 | 8 | 4 | 6 | 9 | 42 | 21 | 44 | 31 | 37 | 49
Injuries | 0 | 0 | 0 | 0 | 1 | 0 | 1 | 2 | 0 | 2 | 0
Injury/ Incident Rate | 0 | 0 | 0 | 0 | 0.11111 | 0 | 0.047619 | 0.045455 | 0 | 0.054054 | 0
FIGURE 49. Reduction & Recycling Incident, Injury & Injury Rate 2012-2022 Sept. 2023

## Slide 52
Rolling & Extrusion Plant Incidents, Injuries / Incident Rate
2012 – 2022
FIGURE 50. Rolling & Extrusion Incident, Injury & Injury Rate 2012-2022 Sept. 2023
Chart: Rolling Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Incidents | 9 | 10 | 11 | 36 | 36 | 44 | 47 | 58 | 38 | 31 | 46
Injuries | 2 | 1 | 4 | 4 | 6 | 2 | 5 | 5 | 3 | 4 | 6
Injury/ Incident Rate | 0.22222 | 0.1 | 0.36364 | 0.11111 | 0.16667 | 0.045455 | 0.10638 | 0.086207 | 0.078947 | 0.12903 | 0.13043
Chart: Extrusion Plant
| 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022
Incidents | 2 | 8 | 13 | 13 | 11 | 10 | 15 | 10 | 6 | 18 | 25
Injuries | 1 | 1 | 3 | 4 | 5 | 0 | 13 | 0 | 2 | 2 | 1
Injury/ Incident Rate | 0.5 | 0.125 | 0.23077 | 0.30769 | 0.45455 | 0 | 0.86667 | 0 | 0.33333 | 0.11111 | 0.04
87%

## Slide 53
Thank you!
@AluminumNews | @ChooseAluminum | @DriveAluminum
Aluminum.org
JOIN THE CONVERSATION